|  | Gravel, Sand | Clean Sand | Clay | Reference | Concrete | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| Hydraulic Conductivity (m/s) | 10-1- 10-3 | 10-2 - 10-5 | 10-8 - 10-11 | Freeze & Cherry (1979) (page 29) | 10-9 (without cracks) | Wong et al. (2009) (page 578) |
|  |  |  |  |  | 10-8 (with microcracks) |  |
| Modulus of Elasticity (ΜPa = 103 KN/m2) | dense | loose | dense | loose | soft | McCarthy (2002) (page 438) | 17,000 – 31,000 (compression) | Gere & Timoshenko (1996) (page 889) |
|  | from 90 |  | from 45 |  |  |  |  |  |
|  | to 180 | from 45 | to 80 | from 9 | 5-0.5 |  |  |  |
|  |  | to 145 |  | to 25 |  |  |  |  |

Gere, J.M. and S.P. Timoshenko (1996). Mechanics of Materials, 4th Ed., Nelson Engineering.

McCarthy, D.F. (2002). Essentials of Soil Mechanics and Foundations, 6th Ed., Prentice Hall.

Wong, H.S., M. Zobel, N.R. Buenfeld and R.W. Zimmerman (2009). Influence of the interfacial transition zone and microcracking on the diffusivity, permeability and sorptivity of cement-based materials after drying, Mag. Concr. Res., 61:8:571-589.

# Text boxes

Ranges of variability of hydraulic conductivity and modulus of elasticity in soils and concrete